DIVISION 04 – MASONRY

SECTION ( 04 0120 )

MAINTENANCE OF UNIT MASONRY – BRICK AND TERRA COTTA

PART 1 – GENERAL

  - SUMMARY

      - Includes, but not limited to:

        - Material and methods for removal of mortar for re-pointing Brick and Terra Cotta.

        - Material and methods for removal of calcium-based stains from Brick and Terra Cotta.

        - Material and methods for restoration - removal of non-calcium based stains from Brick and Terra Cotta.

        - Material and methods for removal of coatings from Brick and Terra Cotta surface.

    - Related Sections:

        - Section 04 0140: ‘Maintenance of Stone Assemblies’

        - Section 04 0200: ‘Unit Masonry’

        - Section 04 2113: ‘Brick Masonry’

        - Section 04 2200: ‘Concrete Unit Masonry’

        - Section 04 4200: ‘Exterior Stone Cladding’

  - REFERENCES

- Definitions:

- Cold Weather, for cleaning purposes, refers to the surface temperature at or below 40° F (4° C) and is expected to remain below for a period of (7) days after cleaning.

- Hot Weather, for cleaning purposes, refers to the surface temperature at or above 90° F (32° C).

- Low Pressure Spray: Under 100 P.S.I. (Pounds per Square Inch)

- High Pressure Spray: Above 800 P.S.I. (Pounds per Square Inch)

- Reference Standards:

  - ACHP: Advisory Council on Historic Preservation.

  - ASTM: American Society for Testing and Materials International.

  - CFR: Code of Federal Regulations.

  - ADMINISTRATIVE REQUIREMENTS

- Pre-testing: testing of cleaning material on all applicable substrates should be conducted prior to full scale cleaning.

  - SUBMITTALS

- Manufacturers Documentation

- Product Data and MSDS for each product submitted;

- Supporting information, i.e. literature as requested.

  - QUALITY ASSURANCE

- Testing

  - For the re-pointing material, clean a mock-up panel or clean an indiscreet area.

  - For each type of stain, clean a 2’ x 2’ section in an indiscreet area.

  - For each type of coating surface, strip a 2’ x 2’ section in an indiscreet area.

  - Allow test area to completely dry prior to evaluating cleaning results.

  - Do not proceed with full scale cleaning until Architect has accepted the cleaning results.

  - DELIVERY, HANDLING AND STORAGE

- Storage and Handling Requirements

- Chemicals may be stored in cold weather temperatures, but should be brought up to 40° F or higher prior to usage.

- Chemicals should be handled according to manufacturers’ safety procedures.

PART 2 – PRODUCTS

  - MATERIALS

- Mortar Removal Materials

- Acid-Based Cleaner: Manufacturers’ standard acidic new masonry cleaner composed of buffered hydrochloric acid

  - EaCo Chem, Inc.: NMD 80

- Non-Hydrochloric Acid Based Cleaner: Manufacturers’ standard non-hydrochloric acidic new masonry cleaner composed of organic salts

- EaCo Chem, Inc.: SOS 50

- Calcium-Based Stain Removal Materials

  - Water Soluble Salts (efflorescence) Remover: Manufacturers’ proprietary cleaner designed to remove calcium chloride (efflorescence) and help prevent its return.

- EaCo Chem, Inc.: EF-Fortless

- EaCo Chem, Inc.: NMD 80

  - Calcium Carbonate (calcite) Remover: Manufacturers’ proprietary two-step system designed to remove calcium carbonate (calcite) deposits.

- EaCo Chem, Inc.: Calcite Presoak followed by NMD 80

  - Calcium Silicate (white scum) Remover: Manufacturers’ proprietary two-step system designed to remove calcium silicate (white scum) deposits.

    - EaCo Chem, Inc.: White Scum Presoak followed by NMD 80

- Restoration - Non-Calcium Based Stain Removal Materials

- Acid-Based Cleaner: Manufacturers’ non-regulated acidic restoration cleaner composed of hydrochloric acid blended with other acids, detergents, wetting agents and inhibitors.

  - EaCo Chem, Inc.: OneRestore

- Ammonium Bifluoride-Based Cleaner: Manufacturers’ standard acidic restoration cleaner composed of ammonium bifluoride blended with other acids, detergents, wetting agents and inhibitors.

  - EaCo Chem, Inc.: GS Restoration

- Coating Removal Materials

- Alkaline-Based Coating Remover: Manufacturers’ standard alkaline-based formulation for removing coatings from limestone.

  - EaCo Chem, Inc.: LCS

- Solvent-Based Coating Remover: Manufacturers’ standard solvent formulation for removing coatings from brick and terra cotta.

  - EaCo Chem, Inc.: AcryliStrip

  - EaCo Chem, Inc.: Graf-Ex

- Low Odor Solvent-Based Coating Remover: Manufacturers’ standard solvent formulation for removing coatings from brick and terra cotta.

  - EaCo Chem, Inc.: Stripsol LO

- Paste Alkaline-Based Coating Remover: Manufacturers standard paste alkaline formulation for removing multiple layers of coatings from limestone.

  - EaCo Chem, Inc.: Stripper Cream

- Paste Solvent-Based Coating Remover: Manufacturers standard paste solvent formulation for removing multiple layers of coatings from limestone.

  - EaCo Chem, Inc.: InStrip

2.02 MANUFACTURER

- Mortar removal cleaner manufacturer contact information: EaCo Chem, Inc.; 765 Commerce Ave, New Castle, PA  16101 – Phone: 724-656-1055, Fax: 724-656-0757 – info@eacochem.com – www.eacochem.com

- Calcium-based stain remover manufacturer contact information: EaCo Chem, Inc.; 765 Commerce Ave, New Castle, PA  16101 – Phone: 724-656-1055, Fax: 724-656-0757 – info@eacochem.com – www.eacochem.com

- Restoration - Non-calcium based cleaner manufacturer contact information: EaCo Chem, Inc.; 765 Commerce Ave, New Castle, PA  16101 – Phone: 724-656-1055, Fax: 724-656-0757 – info@eacochem.com – www.eacochem.com

- Coating remover manufacturer contact information: EaCo Chem, Inc.; 765 Commerce Ave, New Castle, PA  16101 – Phone: 724-656-1055, Fax: 724-656-0757 – info@eacochem.com – www.eacochem.com

PART 3 – EXECUTION

  - RESTORATION CLEANING SPECIALIST

    - Restoration Cleaning Specialist Firms: Subject to compliance with requirements, [provide restoration cleaning specialist firms requirements]

  - PROTECTION

  - Protect adjacent and surrounding surfaces not intended to be cleaned from exposure to the cleaning chemical to prevent damage.

  - Prevent cleaning chemical from coming into contact with people, motor vehicles, landscaping and other building materials that could be harmed by such contact.

  - Follow chemical cleaner and chemical remover manufacturers’ recommendations for personal protection.  Always read product spec sheets for personal protection.

  - MORTAR REMOVAL

- Pre-wet (do not saturate) or flash cool the surface with water.

- Apply acid-based or non-acid based new masonry material in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

- Use a chemical resistant sprayer to apply the restoration material evenly over the entire surface.

- Do not allow new masonry material to dry on the brick or terra cotta surface or any adjacent surface.

- Rinse the new masonry material thoroughly from the surface.  Continue the rinse to the lower levels so no chemical dries on lower levels.

  - CALCIUM-BASED STAIN REMOVAL

- Water Soluble Salts (efflorescence) Removal:

- Apply proprietary cleaner in accordance to manufacturers’ instructions based on pre-tested and pre-approved area.

  - Use an acid resistant sprayer to apply cleaner evenly over the affected areas.

  - The product will foam upon contact with the stains.  When the foaming ceases; apply another application to the affected areas.  Continue re-applying until there is no more foam on contact.

  - Rinse material according to product instructions.

  - Clean the rest of the wall as necessary.

- Calcium Carbonate (calcite) Removal:

- Apply proprietary two-step system in accordance to manufacturers’ instructions based on pre-tested and pre-approved area.

- Use an acid resistant sprayer to apply the first step evenly over the affected areas.  Rinse the runoff before it can set on un-affected areas.

- The product will foam upon contact.  Allow to dwell for a pre-determined time.  Repeat until a scratch test shows the calcite has been softened.

- Use an acid resistant sprayer to apply the second step evenly over the affected areas.

- Rinse material according to product instructions.

- Repeat above steps as necessary.

- Clean the rest of the wall as necessary.

- Calcium Silicate (white scum) Removal:

- Apply proprietary two-step system in accordance to manufacturers’ instructions based on pre-tested and pre-approved area.

  - Use an acid resistant sprayer to apply the first step evenly over the affected areas.  Rinse the runoff before it can set on un-affected areas.

  - The product will foam upon contact.  Allow to dwell for a pre-determined time.

  - Use an acid resistant sprayer to apply the second step evenly over the affected areas.

  - Rinse material according to product instructions.

  - Repeat above steps as necessary.

  - Clean the rest of the wall as necessary.

  - RESTORATION - NON-CALCIUM BASED STAIN REMOVAL

    - Stain removal with acid-based or gelled acid-based restoration material:

        - Pre	-wet (do not saturate) or flash cool the surface with clean water.

        - Apply acid-based and/or gelled acid-based restoration material in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

          - Use an acid resistant sprayer to apply the restoration material evenly over the entire surface.

          - Do not allow the restoration material to dry on the surface or any adjacent surface.

          - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

    - Stain removal with ammonium bifluoride-based restoration material:

        - Pre-wet (do not saturate) or flash cool the surface with clean water.

        - Apply ammonium bifluoride-based restoration material in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

          - Use an acid resistant sprayer to apply the restoration material over the intended surface.

          - Do not allow the restoration material to dry on the surface or any adjacent surface.  Keep the restoration material off of any surface not suitable for this type of material.

          - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

  - COATING REMOVAL

- Coating removal with alkaline-based coating remover:

- Use a caustic resistant sprayer to apply coating remover to a dry surface.

- Allow coating remover to sit on the surface for a period of time determined in pre-tested and pre-approved area.

- Rinse coating remover and removed coating from the surface using high pressure.  Continue the rinse to the lower levels to prevent coating from setting on those levels.

  - Dispose of coating waste in accordance to local regulations.

- Apply acid-based, gelled acid-based or ammonium biluoride-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

  - Do not allow restoration material to dry on the surface or any adjacent surface.

  - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

- Coating removal with solvent-based coating remover:

- Use a solvent compatible sprayer to apply the coating remover to a dry surface.

- Allow coating remover to sit on the surface for a period of time determined in pre-testing and pre-approved areas.

- Rinse coating remover and loosened coating from the surface using high pressure.  Continue the rinse to the lower levels to prevent coating from setting on those levels.

  - Dispose of coating waste in accordance to local regulations.

- Apply acid-based, gelled acid-based or ammonium biluoride-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

  - Do not allow restoration material to dry on the surface or any adjacent surfaces.

  - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

- Coating removal with paste alkaline-based coating remover.

- Use a caustic compatible sprayer or roller to apply the coating remover to a dry surface.

- Allow coating remover to sit on the surface for a period of time determined in pre-testing and pre-approved areas.

- Rinse coating remover and loosened coating from the surface using low pressure first to collect coating residue at the base of the wall.  Follow with a high pressure rinse to remove remaining coating from the wall.  Continue the rinse to the lower levels to prevent coating from setting on those levels.

- Dispose of coating waste in accordance to local regulations.

- Apply acid-based, gelled acid-based or ammonium biluoride-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

  - Do not allow restoration material to dry on the surface or any adjacent surfaces.

  - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

- Coating removal with paste solvent-based coating remover.

- Use a solvent compatible roller or brush to apply the coating remover to a dry surface.

- Allow coating remover to sit on the surface for a period of time determined in pre-testing and pre-approved areas.

- Rinse coating remover and loosened coating from the surface using low pressure first to collect coating residue at the base of the wall.  Follow with a high pressure rinse to remove remaining coating from the wall.  Continue the rinse to the lower levels to prevent coating from setting on those levels.

  - Dispose of coating waste in accordance to local regulations.

- Apply acid-based, gelled acid-based or ammonium bifluoride-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

  - Do not allow restoration material to dry on the surface or any adjacent surfaces.

  - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

  - FINAL CLEANING

- Clean site of all unused cleaning material, residues, rinse water, wastes and protection material in accordance with federal and local environmental regulations.

END OF SECTION