DIVISION 04 – MASONRY

SECTION ( 04 0140 )

MAINTENANCE OF STONE ASSEMBLIES - LIMESTONE

PART 1 – GENERAL

  - SUMMARY

      - Includes, but not limited to:

        - Material and methods for removal of surface stains from Limestone.

        - Material and methods for removal of deep set stains from Limestone.

        - Material and methods for removal of dimentional stains from Limestone.

        - Material and methods for removal of graffiti or multiple layers of paint from Limestone surface.

    - Related Sections:

        - Section 04 0120: ‘Maintenance of Unit Masonry’

        - Section 04 4200: ‘Exterior Stone Cladding’

  - REFERENCES

- Definitions:

- Cold Weather, for cleaning purposes, refers to the surface temperature at or below 40° F (4° C) and is expected to remain below for a period of (7) days after cleaning.

- Hot Weather, for cleaning purposes, refers to the surface temperature at or above 90° F (32° C).

- Low Pressure Spray: Under 100 P.S.I. (Pounds per Square Inch)

- High Pressure Spray: Above 800 P.S.I. (Pounds per Square Inch)

- Reference Standards:

  - ACHP: Adivisory Council on Historic Preservation.

  - ASTM: American Society for Testing and Materials International.

  - CFR: Code of Federal Regulations.

  - ADMINISTRATIVE REQUIREMENTS

- Pre-testing: testing of cleaning material on all applicable substrates should be conducted prior to full scale cleaning.

  - SUBMITTALS

- Manufacturers Documentation

- Product Data and MSDS for each product submitted;

- Supporting information, i.e. literature as requested.

  - QUALITY ASSURANCE

- Testing

  - For each type of stain, clean a 2’ x 2’ section in an indiscreet area.

  - For each type of coating surface, strip a 2’ x 2’ section in an indiscreet area.

  - Allow test area to completely dry prior to evaluating cleaning results.

  - Do not proceed with full scale cleaning until Architect has accepted the cleaning results.

  - DELIVERY, HANDLING AND STORAGE

- Storage and Handling Requirements

- Chemicals may be stored in cold weather temperatures, but should be brought up to at least 40° F prior to usage.

- Chemicals should be handled according to manufacturers’ safety procedures.

PART 2 – PRODUCTS

  - MATERIALS

- Restoration Materials

- Acid-Based Cleaner: Manufacturers’ non-regulated acidic restoration cleaner composed of hydrochloric acid blended with other acids, detergents, wetting agents and inhibitors.

  - EaCo Chem, Inc.: OneRestore

- Gelled Acid-Based Cleaner: Manufacturers’ standard gelled acidic restoration cleaner composed of hydrochloric acid blended with other acids, detergents, wetting agents and inhibitors.

  - EaCo Chem, Inc.: OneRestore GEL

- Paste Alkaline-Based Cleaner: Manufacturers standard paste alkaline formulation for removing thick surface stains from limestone.

  - EaCo Chem, Inc.: Stripper Cream

- Coating Removal Materials

- Alkaline-Based Coating Remover: Manufacturers’ standard alkaline formulation for removing coatings from limestone.

  - EaCo Chem, Inc.: LCS

- Solvent-Based Coating Remover: Manufacturers standard solvent formulation for removing coatings from limestone.

  - EaCo Chem, Inc.:  AcryliStrip

  - EaCo Chem, Inc.:  Graf-Ex

- Paste Alkaline-Based Coating Remover: Manufacturers standard paste alkaline formulation for removing multiple layers of coatings from limestone.

  - EaCo Chem, Inc.: Stripper Cream

- Paste Solvent-Based Coating Remover: Manufacturers standard paste solvent formulation for removing multiple layers of coatings from limestone.

  - EaCo Chem, Inc.: InStrip

2.02 MANUFACTURER

- Restoration cleaner manufacturer contact information: EaCo Chem, Inc.; 765 Commerce Ave, New Castle, PA  16101 – Phone: 724-656-1055, Fax: 724-656-0757 – info@eacochem.com – www.eacochem.com

- Coating remover manufacturer contact information: EaCo Chem, Inc.; 765 Commerce Ave, New Castle, PA  16101 – Phone: 724-656-1055, Fax: 724-656-0757 – info@eacochem.com – www.eacochem.com

PART 3 – EXECUTION

  - RESTORATION CLEANING SPECIALIST

    - Restoration Cleaning Specialist Firms: Subject to compliance with requirements, [provide restoration cleaning specialist firms requirements]

  - PROTECTION

  - Protect adjacent and surrounding surfaces not intended to be cleaned from exposure to the cleaning chemical to prevent damage.

  - Prevent cleaning chemical from coming into contact with people, motor vehicles, landscaping and other building materials that could be harmed by such contact.

  - Follow cleaner manufacturers’ recommendations for personal protection.

  - SURFACE AND DEEP SET STAIN REMOVAL

- Pre-wet (do not saturate) or flash cool the surface with water.

- Apply acid-based and/or gelled acid-based restoration material in accordance to manufacturers’ instructions based on pre-tested and pre-approved area.

- Use an acid resistant sprayer to apply the restoration material evenly over the entire surface.

- Do not allow restoration material to dry on the limestone surface or any adjacent surface.

- Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

  - DIMENTIONAL STAIN REMOVAL

- Pre-wet (do not saturate) or flash cool the surface with water.

- Apply paste alkaline-based cleaner in accordance to manufacturers’ instructions based on pre-tested and pre-approved area.

- Use a caustic compatible sprayer or roller to apply the restoration material over the areas with the dimentional stains.

- Allow restoration material to sit on limestone surface for a pre-determined time.  Depending on severity, extended dwell time may be required.

- Rinse restoration material thoroughly from surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

- Apply acid-based and/or gelled acid-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved area.

      - Use an acid resistant sprayer to apply the restoration material evenly over the entire surface.

      - Do not allow restoration material to dry on the limestone surface or any adjacent surface.

      - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

  - COATING REMOVAL

- Coating removal with alkaline-based coating remover:

- Use a caustic compatible sprayer to apply coating remover to a dry surface.

- Allow coating remover to sit on the surface for a period of time determined in pre-tested and pre-approved area.

- Rinse coating remover and removed coating from the surface using high pressure.  Continue the rinse to the lower levels to prevent coating from setting on those levels.

  - Dispose of coating waste in accordance to local regulations.

- Apply acid-based and/or gelled acid-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

  - Do not allow restoration material to dry on the limestone surface or any adjacent surface.

  - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

- Coating removal with solvent-based coating remover:

- Use a solvent compatible sprayer to apply coating remover to a dry surface.

- Allow coating remover to sit on the surface for a period of time determined in pre-tested and pre-approved area.

- Rinse coating remover and removed coating from the surface using high pressure.  Continue the rinse to the lower levels to prevent coating from setting on those levels.

  - Dispose of coating waste in accordance to local regulations.

- Apply acid-based and/or gelled acid-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

  - Do not allow restoration material to dry on the limestone surface or any adjacent surface.

  - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

- Coating removal with paste alkaline coating remover.

- Use a caustic compatible sprayer or roller to apply the coating remover to a dry surface.

- Allow coating remover to sit on the surface for a period of time determined in pre-testing and pre-approved areas.

- Rinse coating remover and loosened coating from the surface using low pressure first to collect coating residue at the base of the wall.  Follow with a high pressure rinse to remove remaining coating from the wall.  Continue the rinse to the lower levels to prevent coating from setting on those levels.

- Dispose of coating waste in accordance to local regulations.

- Apply acid-based and/or gelled acid-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

  - Do not allow restoration material to dry on the limestone surface or any adjacent surfaces.

  - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

- Coating removal with paste solvent coating remover.

- Use a solvent compatible roller or brush to apply the coating remover to a dry surface.

- Allow coating remover to sit on the surface for a period of time determined in pre-testing and pre-approved areas.

- Rinse coating remover and loosened coating from the surface using high pressure.  Continue the rinse to the lower levels to prevent coating from setting on those levels.

  - Dispose of coating waste in accordance to local regulations.

- Apply acid-based and/or gelled acid-based restoration material if needed in accordance to manufacturers’ instructions based on pre-tested and pre-approved areas.

  - Do not allow restoration material to dry on the limestone surface or any adjacent surfaces.

  - Rinse the restoration material thoroughly from the surface.  Continue the rinse to the lower levels to prevent soil or material from setting on those levels.

  - FINAL CLEANING

- Clean site of all unused cleaning material, residues, rinse water, wastes and protection material in accordance with federal and local environmental regulations.

END OF SECTION