DIVISION 03 – CONCRETE

SECTION ( 03 4713 )

TILT-UP CONCRETE

PART 1 – GENERAL

  - SUMMARY

      - Includes, but not limited to:

        - Material and methods for removal of mortar and/or jobsite debris from Tilt-Up Concrete surface.

    - Related Sections:

        - Section 03 3000: 		‘Cast-in-Place Concrete’

        - Section 03 4500: 		‘Precast Architectural Concrete’

        - Section 04 2113: 		‘Brick Masonry’

        - Section 04 4200: 		‘Exterior Stone Cladding’

        - Section 04 4313.13: 	‘Anchored Stone Masonry Veneer’

        - Section 04 4313.16:	‘Adhered Stone Masonry Veneer’

        - Section 04 7200:		‘Cast Stone Masonry’

  - REFERENCES

- Definitions:

- Cold Weather, for cleaning purposes, refers to the surface temperature at or below 40° F (4° C) and is expected to remain below for a period of (7) days after cleaning.

- Hot Weather, for cleaning purposes, refers to the surface temperature at or above 100° F (38° C).

- Low Pressure Spray: Under 100 P.S.I. (Pounds per Square Inch)

- High Pressure Spray: Above 800 P.S.I. (Pounds per Square Inch)

- Reference Standards:

  - ADMINISTRATIVE REQUIREMENTS

- Pre-testing: testing of cleaning material on all applicable substrates should be conducted prior to full scale cleaning.

  - SUBMITTALS

- Manufacturers Documentation

- Product Data and MSDS for each product submitted;

- Supporting information, i.e. literature as requested.

  - QUALITY ASSURANCE

- Mockup Panel

  - Clean mockup panel using the chemical manufacturers’ recommended cleaning method.

  - Allow mockup panel to completely dry prior to evaluating cleaning results.

  - Do not proceed with full scale cleaning until Architect has accepted the cleaning results.

  - DELIVERY, HANDLING AND STORAGE

- Storage and Handling Requirements

- Chemicals may be stored in cold weather temperatures, but should be brought indoors prior to usage.

- Chemicals should be handled according to manufacturers’ safety procedures.

PART 2 – PRODUCTS

  - MATERIALS

- Cleaning Materials

- Acid-Based Cleaner: Manufacturers’ standard acidic new masonry cleaner composed of buffered hydrochloric acid

  - NMD 80 manufactured by EaCo Chem, Inc.; New Castle, PA www.eacochem.com

- Non-hydrocloric acid Based Cleaner: Manufacturers’ standard non-hydrocloric acid new masonry cleaner composed of organic salts

  - SOS 50 manufactured by EaCo Chem, Inc.; New Castle, PA www.eacochem.com

2.02 MANUFACTURER

- New masonry cleaner manufacturer contact information: EaCo Chem, Inc.; 765 Commerce Ace, New Castle, PA  16101 – Phone: 724-656-1055, Fax: 724-656-0757 – info@eacochem.com – www.eacochem.com

PART 3 – EXECUTION

  - CONCRETE CLEANING SPECIALIST

    - Concrete Cleaning Specialist Firms: Subject to compliance with requirements, [provide concrete cleaning specialist firms requirements]

  - PROTECTION

  - Protect adjacent and surrounding surfaces not intended to be cleaned from exposure to the cleaning chemical to prevent damage.

  - Prevent cleaning chemical from coming into contact with people, motor vehicles, landscaping and other building materials that could be harmed by such contact.

  - Follow new masonry cleaner manufacturers’ recommendations for personal protection.

  - APPLICATION

- Dilute cleaning material as directed by manufacturers’ recommendations per Product Data sheet.

- For mortar removal, allow mortar to cure for a period of 7 days before beginning the cleaning process can begin.

- Beginning from the top of the wall, lightly pre-wet or pre-cool the wall;

- Begin applying cleaning material from the top to bottom, using even, overlapping passes to ensure full coverage of chemical on the surface;

  - Apply cleaning material to the entire drop or section of wall that can be cleaned without allowing the chemical to dry on the surface.

- After the first application of cleaning material, scrape the large chunks with a long handled scraper from the first 8 feet of wall;

  - Use a scraper in accordance to masonry manufacturers’ requirements.

- Check smears and tags to see if they crumble easily;

- If needed, repeat application to melt remaining residue and extend dwell time;

- After re-application, scraping can be done further down the wall;

- Once smears and tags crumble easily, begin rinsing from top down.  A thorough rinse is necessary to avoid leaving any cleaning material on the surface or in the masonry unit.

  - Use long even strokes that overlap each other.

  - Rinse pressure is determined by the masonry manufacturers’ requirements.  Color sensitive surfaces should always be rinsed with low pressure.

- For jobsite debris removal, follow cleaning material manufacturers’ dilutions and instructions per “Tilt-Up Concrete” section of the Product Data sheet.

  - FINAL CLEANING

- Clean site of all unused cleaning material, residues, rinse water, wastes and protection material in accordance with federal and local environmental regulations.

END OF SECTION